GE Silicone Sealants 222Rn Emanation Measurement
H. Ryott Glayzer
Lab Assistant
SD Mines

---
GE All-Purpose Sealant
- GE All-Purpose Sealant has a rate of
  - This measurement is taken from 465 hours of usable data
  - The uncertainties in this figure were calculated separately for top and bottom errors in order to provide a more conservative estimate
- A sample with ~200cm2 of surface area was emanated six times throughout Summer 2023 at SD Mines
  - Four of those runs contained useful data
- The emanation rate of this sealant is sufficiently low for SuperCDMS
0.00 binom{+0.02}{-0.00} mBq

---
Rate vs. Time, Run 717
This run indicates a rate of
This is based solely off of the 214Po rate because of low resolution between 218Po and 210Po peaks which caused 210Po events to ‘spill over’ into the 218Po ROI which makes the 218Po rate unreliable
0.00 binom{+0.03}{-0.00} mBq

---
Rate vs. Time, Run 720
This run indicates a rate of
This is based solely off of the 214Po rate because of low resolution between 218Po and 210Po peaks which caused 210Po events to ‘spill over’ into the 218Po ROI which makes the 218Po rate unreliable
0.00 binom{+0.54}{-0.00} mBq
0.00

---
Rate vs. Time, Run 721
This run indicates a rate of
This is based solely off of the 214Po rate because of low resolution between 218Po and 210Po peaks which caused 210Po events to ‘spill over’ into the 218Po ROI which makes the 218Po rate unreliable
0.00 binom{+0.02}{-0.00} mBq

---
Rate vs Time, Run 722
This run indicates a rate of
This is based solely off of the 214Po rate because of low resolution between 218Po and 210Po peaks which caused 210Po events to ‘spill over’ into the 218Po ROI which makes the 218Po rate unreliable
0.00 binom{+0.10}{-0.00} mBq

---
GE Advanced Sealant
0.00 binom{+0.03}{-0.00} mBq
- GE Advanced Sealant has a rate of
  - This measurement is taken from 163 hours of usable data
- A sample with ~200cm2 of surface area was emanated one time in September 2023 at SD Mines
  - This run resulted in 163 hours of usable data
- The emanation rate for this sealant is sufficiently low for SuperCDMS purposes

---
Rate vs Time, Run 730
Combined Rate of 214Po and 218Po rates gives a rate of
The combined rate was chosen because there was good resolution between the 210Po and 218Po ROIs
0.00 binom{+0.01}{-0.00} mBq

---
Summary
- Both Sealants assayed are sufficiently low for use in SuperCDMS
- Both sealants assayed have a sufficient amount of usable data and no additional runs are necessary